|  |  |  |  |
| --- | --- | --- | --- |
| **ULTRA Q7 SUPER DIESEL ENGINE OIL**  **SAE 15W-40** | | | |
| **PERFORMANCE PROFILE** | |  |
| API CH4/SL |  |  |
| **APPLICATION** | | |
| |  | | --- | | A superior quality, high performance diesel engine oil designed for the most severe performance requirements of highly powered turbocharged engines of leading Japanese, European and American Manufactures. Specially suited for use in mixed fleets, commercial road transport and off the road vehicles and plants. | | | |
| KEY FEATURES | | |
| * Exceptional thermal stability at high temperature * Extremely high control over wear, rust and corrosion to ensure long life of moving parts. * Outstanding lubrication powers in all seasons * Improved fuel economy and filterability * Longer maintenance intervals and oil change period * Excellent fluidity at low temperature ensures good starting * Excellent protection against oxidation, foaming, low temperature sludge and high temperature deposits * Properly balanced detergency and dispersancy ensures a clean engine | | |

|  |  |  |
| --- | --- | --- |
| **TECHNICAL DATA** | | |
| **CHARACTERISTICS** | **TEST METHOD** | **TYPICAL VALUE** |
| **15W-40** |
| Density at 15 oC, Kg/L | ASTM D1298 | 0.886 |
| Viscosity at 100 oC, cSt | ASTM D445 | 14.5 |
| Viscosity Index | ASTM D2270 | 135 |
| Flash Point, COC, oC | ASTM D92 | 234 |
| Pour Point, oC | ASTM D97 | -30 |
| TBN, mgKOH/g | ASTM D2896 | 11.5 |